## Slide 1: Simultaneous Determination of Additive Concentration in Rubber using ATR-FTIR Spectroscopy
Stephen Merrimana, Dinesh Chandrab, Marc Borowczakb, Ali Dhinojwalaa, David Benkob
School of Polymer Science and Polymer Engineering
a
b
Notes: 30 talk total

## Slide 2: Motivation
Anthoine, B.H.; Ignatz-Hoover, T. Int. Polym. Sci. Technol. 32 (11) 1-13
Tracking additives (curing agents, antioxidants, antiozonants, etc.) between rubber compounds and throughout a tire is necessary to assess and optimize performance.
Experimentally monitoring additive concentrations is difficult and time consuming.
  Component isolation and extraction.
Preferred method:
  Measure additive concentrations directly on rubber.

## Slide 3: Attenuated Total Reflectance (ATR) Infrared (IR) Spectroscopy
IR Light Input
IR Light Output
Detector
Sample
Conventional / Transmission FT-IR Spectroscopy
Sample
Detector
IR Light Input
Crystal
Attenuated Total Reflectance (ATR) FT-IR Spectroscopy
Spectral Database. https://spectrabase.com/spectrum/3gHGPFgWrKC
Methanol
Spectral Database. https://spectrabase.com/spectrum/3gHGPFgWrKC
https:/bruker.com

## Slide 4: Quantification using ATR spectroscopy
Considering three antioxidants/antiozonants (“antidegradents”) of similar chemical structure.
Rubber A (Silica filled NR)
Rubber B (C-black filled NR:PBD blend)
Beer’s law:
Absorbance
Molar absorptivity
Pathlength
Concentration
Merriman, S. et al. Spectrochim. Acta A Mol. Biomol. 281 (121614)

## Slide 5: Beer’s Law Validation
Baseline
Integration
Baseline
Antidegradent absorbance closely matches Beer’s law
Merriman, S. et al. Spectrochim. Acta A Mol. Biomol. 281 (121614)
Rubber A (Silica filled NR)
Rubber B (C-black filled NR:PBD blend)

## Slide 6: Classical Least Squares Analysis
Beer’s law:
One component
Beer’s law:
components
Peak 1:
Peak 2:
Peak 3:
Only total antidegradent concentration can be determined.
Merriman, S. et al. Spectrochim. Acta A Mol. Biomol. 281 (121614)
Rubber A (Silica filled NR)
Rubber B (C-black filled NR:PBD blend)

## Slide 7: Partial Least Squares Analysis
Partial least squares (PLS) multivariate statistical approach:
  Consider the absorbance at every wavenumber within defined spectral regions (lots of data points!) rather than 3 discrete peak areas.
  Construct a predictive model taking into account each point.
  Well suited for analysis of spectral data.
Each antidegradent can be individually quantified to ~0.15 wt%
Merriman, S. et al. Spectrochim. Acta A Mol. Biomol. 281 (121614)

## Slide 8: Conclusions
Antidegradent IR absorbance in rubber closely follows Beer’s law for 0-~4.5wt% (0-7 PHR).
Classical least squares (3-peak area) quantification method predicts total antidegradent wt%, but not individual concentrations.
Partial least squares (PLS) quantification method predicts each antidegradent individually to within ~0.15 wt%.
Takeaways
  Chemical quantification directly on fully formulated rubber using IR absorption spectra is possible.
  The method demonstrated could be extended to other additives and/or other systems and could be used to track migration, blooming, reactions, etc.
  Compared to traditional methods, IR spectra collection is direct, non-destructive, spatially-resolved, and rapid.
https://doi.org/10.1016/j.saa.2022.121614
Full details of the project:

## Slide 9: Questions

## Slide 10: Supplemental Slides

## Slide 11: Problems with IR absorption-based quantification
Mayerhöfer, T. G., et al. ChemPhysChem 2016, 17, 1-9.
Mayerhöfer, T. G., et al. ChemPhysChem 2020, 21, 2029-2046.
Antidegradents of similar chemical structure show similar spectral signatures and overlapping peaks.
Beer’s law is highly idealized: not applicable in general to all systems.
  Especially true for larger absorbance and samples with non-homogenous optical properties (i.e., complex refractive index).
Concentration
Merriman, S. et al. Spectrochim. Acta A Mol. Biomol. 281 (121614)

## Slide 12: Rubber Formulations